## Slide 1: FP4470 viscosity
Juliane Junesch, AEE TCS
Henkel Düsseldorf, Germany
2021-09-17

## Slide 2: FP4470
3DPlus noticed viscosity changes over time when it is heated (50C).
Therefore they would like to have viscosity curve at 50°C for 2 hours and an other curve at 25°C.
background

## Slide 3: Equipment & Settings
The viscosity was measured with Anton Paar Rheometer MCR302 H-PTD200
Settings were copied from IFX
  Parallel Plate 25mm
  Gap 0.2mm Temperature: 25°C, 50°C
  Hold 10 min without shear force
  Shear rates: 1s-1
  Time 2 hours
Rheometer

## Slide 4: FP4470
Viscosity over time

## Slide 5: Conclusion
The viscosity of FP4410 was tracked over 2hours at 25°C and 50°C
It stayed stable over this time
  @25°C is remained at 25.0 Pas
  @50°C there is a slight increase (from 2.8Pas to 3.1 Pas)

## Slide 6: THANK YOU