## Slide 1
NanoProof® 3 Series
3M™ Novec™ Engineered Grade Coatings Replacement
www.aculon.com
Aculon® Confidential Information

## Slide 2: AGENDA
AGENDA
Introduction
NanoProof® Overview
NanoProof 3 Series -3M™ Product Comparison (1700, 1900, 2700)
Summary
Questions & Discussion

## Slide 3: OUR GOAL
Aculon® uses its expertise in surface modiﬁcation technologies to enable customers to make better products by being fast, innovative & responsive.
Together we create winning products!

## Slide 5
Founded 2004
Expertise
Develop & produce surface solutions to modify a broad variety of surfaces (metals, metal oxides, ceramics, glass, polymers)
Functionality
Hydrophobic, superhydrophobic, oleophobic, hydrophilic, oleophilic anti-ﬁngerprinting, adhesion promotion
Treatments
Thin, easy to apply (no vacuum chambers),
often no cure, safe, non-toxic, and offer green & VOC exempt options.
-Over 100 Products
Differentiation
Create proprietary innovative treatments & willingness to work with customer to solve problems
Focus areas
Electronics,
Oil & Gas,
Medical,
Specialty
Business Model
Optimize custom surface treatment solutions, produce and sell treatment chemistry, treat parts for customers if required
-ISO 9001
Knowledge
- >40 Patents granted.
-Invested 100,000’s hours on 1000’s projects.
-Smart (numerous Chemists with PhD’s & Masters Degrees, Electrical & Mechanical Engineers)
Global
Locations
San Diego (HQ, Lab & Manufacturing),
Shanghai, Singapore, Dusseldorf, Amsterdam, Dallas, Houston
Distributors
ACULON® OVERVIEW- Founded in 2004

## Slide 6: MANY SURFACE MODIFICATION PLATFORMS
Oleophilic
Transition Metal Complexes
Hydrophilic
Self Assembled Monolayers of Phosphonates
(SAMPs)
Polymeric Organometallics
Organometallic
Surface Polymer Growth

## Slide 7: BROAD PORTFOLIO
Surface Cleaners
PRODUCT GROUPS
Attraction treatments
Anti Fingerprinting Treatments
Surface Primers
Waterprooﬁng Treatments
Hard Coats
Adhesion promotion
FUNCTIONALITIES
Superhydrophobic
Oleophobic
Hydrophilic
Superhydrophilic
Anti-ﬁngerprinting
Repellency treatments
Hydrophobic

## Slide 8: ACULON SURFACE PROPERTIES ADJUSTMENTS AT A GLANCE:
Aculon Treatment Examples
Hydrophilicity
Oleophobicity
Hydrophobicity & Super-Hydrophobicity
Application Examples:
Easy Clean & Anti-Fingerprint
(Electronics)
Waterprooﬁng
Untreated Surface
Adhesion Promotion
Particle Treatment
Membranes Treatment
ACULON – BECAUSE SURFACES MATTER!

## Slide 9
Surface Modiﬁcation
Medical
Barrier protection (Electronics & Automotive)
Metal Treatment (Electronics & Industrial)
Enhanced Oil Recovery
Anti- Fingerprinting
Membranes
Anti-Fouling
EXPERTISE AND PLATFORMS

## Slide 10
Electronics
Medical
Energy
Specialty - Other
ACULON® FOCUSES

## Slide 11
NanoClear®
SMT Stencil Nano-Coating
Epoxy & Underﬁll Control
Prevent adhesive ﬂow out
NanoProof®
Electronics Protection
Adhesion Promotion
Improve Bond Strength
Anti-FingerPrint Coatings
Hide appearance of prints
Test Pin Repellency Coatings
Increase Test Pin Lifetime
ELECTRONICS

## Slide 12
In real life, electronic devices are often damaged
Device dropped in pool or even toilet
Unit exposed to outdoor
environment – dust, rain, humidity
Household appliances exposed water during operations
Equipment (industrial and medical) exposed to dirty and wet working environment
ELECTRONICS PROTECTION

## Slide 13
Award winning liquid applied electronics protection technology
Aculon® NanoProof® Series launched in 2010 provides protection from dust & humidity all the way to full water immersion
Utilize proprietary technology
Application equipment affordable and readily available
Range of treatments available to meet IPX3 to IPX8.
NANOPROOF® ELECTRONICS PROTECTION
Aculon technology used on over 1 million EV’s

## Slide 14
NanoProof® Series | IPX | In-Line | Non-Toxic | Push Through | Flexible | Green/VOC Exempt*
1 | 3 |  |  |  |  | 
5 | 5 |  |  |  |  | 
8 | 8 |  |  |  |  | 
X | 8 |  |  |  |  | 
12 | 8 |  |  |  |  | 
15 | 8 |  |  |  |  | 
* Conforms with US EPA or China regulations
CURRENT NANOPROOF® SERIES FEATURES

## Slide 15
Continuous Process
Eliminate slow & cumbersome batch deposition solutions
Flexible liquid solutions include dip, spray, & dispense
Performance & Electrical Isolation
Industry leading electrical isolation.
IPX8 level performance with minimal material utilization.
Thin & Tight Tolerance
IPX8 as thin as 30uM suitable for extremely tight tolerance applications.
Selective application protects sensitive components close to “keep out” areas.
Coat Connectors
Push Through Connectivity allows for protection of sensitive connection components.
Eliminate masking and mechanical gasketing previously required.
Easy Application
Reduce process time with on target & uniform thickness in one / two passes.
Eliminate time consuming vac dep or multiple application passes for target thickness
Uniform & Protects Edges
Consistent coverage across all components with no slumping, even edges.
Eliminate failures due to non-uniform edge coverage
NANOPROOF® ADVANTAGES

## Slide 16: NanoProof® 3 series offers direct replacements to 3M™ Novec™ products.
NanoProof® 3 series offers anti-wetting, anti-stiction, chemical protection, corrosion protection, and moisture protection for PCBs and electrical components.
NanoProof® 3 Series benefits
“Drop-in replacement”
Offered through distributors
Contains UV tracer
Cost effective and in many cases lower cost
INTRODUCING NANOPROOF® 3 SERIES

## Slide 17
PACKAGING
40 mL
1 Liter
1 kg
1 Gallon
5.4 kg
4 Gallon
20 kg

## Slide 18: NANOPROOF 3 - TECHNOLOGY APPLICATION
3M™ Novec™ Product | NanoProof® Alternatives
 | NanoProof® 3-01
3M™ Novec™ 1700 | NanoProof® 3-02
3M™ Novec™ 1702 | NanoProof® 3-002
3M™ Novec™ 1710 | NanoProof® 3-10
3M™ Novec™ 1720 | NanoProof® 3-001X –(LEDs)
3M™ Novec™ 1902 | NanoProof® 3-02
3M™ Novec™ 1904 | NanoProof® 3-04
3M™ Novec™ 1908 | NanoProof® 3-08
3M™ Novec™ 2704 | NanoProof® 3-04
3M™ Novec™ 2708 | NanoProof® 3-08
3M™ Novec™ 7100 | Aculon® 3 Series-Extender
NANOPROOF® 3 – NOVEC™ REPLACEMENTS

## Slide 19
Flexible coating processes make conversion easy to implement.
Spray
Dispense
Dip
NANOPROOF® 3 – TECHNOLOGY APPLICATION

## Slide 20
 | 1700 | 1702 | 1710
Solids | Fluoroacrylate 2% | Fluoroacrylate 0.2% | Fluoroacrylate 10%
Solvent | 7100DL |  | 
Appearance | Clear |  | 
Density | 1.5 g/mL |  | 
Viscosity | 0.91 cP | 0.63 cP | 4.3 cP
Boiling Point | 61°C |  | 
Flash Point | None |  | 
Environmental | Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine |  | 
Shelf Life | 4 yrs in unopened package from manufacture date |  | 
Thickness | 0.1-1 µm | <100 nm | 0.1-1 µm
Chem Resistance | Resists a variety of solvents/chemicals, dissolves in acetone |  | 
Tg | 44°C |  | 
Therm. Stability | 175°C for 24 hours |  | 
Contact Angles | WCA / OCA: 105° / 65° |  | 
Refractive Index | 1.39 |  | 
Solder Thru Repairability | Yes |  | 
Non-Flammability | Meets UL 94 V-0 |  | 
Coef. of Therm. Expn. | 70 µm/(m·°C) |  | 
Therm. Cond. | 0.1 W/m*K |  | 
Diel. Bd Strength | 2000 V/mil |  | 
Cure | None |  | 
Removable | Yes |  | 
NANOPROOF® 3 vs NOVEC™ 1700 SERIES
3-02 | 3-002 | 3-10
Fluoroacrylate 2% | Fluoroacrylate 0.2% | Fluoroacrylate 10%
Aculon 3 Series Exyender |  | 
Light Green |  | 
1.5 g/mL |  | 
<20 cP |  | 
In process, 56-61°C estimate |  | 
None |  | 
Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine |  | 
2 yrs in unopened package from manufacture date |  | 
0.2-2 µm | 0.1-1 µm | 0.25-6 µm
Resists a variety of solvents/chemicals. Attacked by fluorosolvents and ketones |  | 
~95°C from peak on DSC |  | 
Stable in 175°C for 24 hours |  | 
WCA / OCA: 120° / 80° |  | 
n=1.376 @ 632.8 nm |  | 
Yes |  | 
Meets UL 94 V-0 |  | 
In Process |  | 
In Process |  | 
3600 V/mil |  | 
None |  | 
Yes |  | 

## Slide 21
 | 7100
Viscosity | <5 cP
Boiling Point | 61°C
Freezing Point | -135°C
Flash Point | None
Specific Gravity | 1.52 g/mL
Shelf Life | 2 yrs (unopened container)
ACULON® FS-Extender vs NOVEC™ 7100
3 Series-Extender
<1 cP
TBD, Estimate 56-61°C
<-81°C
None
1.5 g/mL
2 yrs (unopened container)

## Slide 22
FAQ
How durable is the coating? | Safe for handling but not abrasion resistant.
What is the targeted thickness? | Target thickness is application dependent.
How can NanoProof 3 be applied? | NanoProof 3 can be dipped, sprayed, and needle dispensed.
Is NanoProof 3 flammable? | No.
Is NanoProof 3 toxic? | No.
Is NanoProof 3 VOC-free? | NanoProof 3 is VOC-exempt in certain countries.
What is the shelf-life? | Recommended storage is in a cool, dry environment (less than 40C). Keep containers tightly sealed. Keep out of sunlight or heat sources. Shelf life for this product is 2 years from the manufacture date in a sealed container.
What are the cure requirements? | NanoProof 3 does not require heat curing. This coating cures at room temperature in less than 5 minutes.
Any compatibility issues with epoxy? | NanoProof 3 may delaminate or apply unevenly on epoxy.
Any specific equipment required? | No. Aculon has a strong relationship with equipment manufacturers such as Nordson, PVA, etc.
How do you measure hydrophobicity and oleophobicity with NanoProof 3? | NanoProof 3 will show water contact angles greater than 110 and oil contact angles greater than 70.
How do you QC the material once applied? | Area coverage can be evaluated visually with the UV Tracer feature - if there are thin layers or areas that are untreated, you can touch up those spots with additional chemistry. You can also measure thicknesses, we use a filmetrics machine.
Do boards need to be cleaned before treatment? | Yes. If there is no clean flux, we recommend using a cleaner. Dust and debris may be removed using air pressure.
What level protection does NP 3 provide? | IPX Level 5/6
Is selective deposition possible? | Yes, masking is not required but can be implemented.
Is NanoProof 3 a flexible coating? | Yes. If less than 1um thick,
Are there any packaging restrictions? | No.
Any consequences if over applied? | Over application may lead to cracking or blistering.
Any keep out areas? | You will not want to coat contacts. This coating is insulative and may create impedance.
Any supply chain risks? | No, multiple sources for the carrier solvent and raw materials.
Is this REACH/RoHS Compliant? | Yes, all Aculon products are REACH/RoHS Compliant.
Is this coating UV stable? | No, will degrade overtime
What is the min thickness after drying for salt water protection? | n/a wont work for full immersion
Does the thickness of the coating correlate to the protection performance (is thicker better)? | Yes
Are there any risks to solvent trapping? | Always a risk, however materials are low enough concentration and the material does not skin over so this would be highly unlikely.
Does the application process have to be done in a ventilated fume hood? | No
If the PCB has sharp edges, will it impact the edge coverage? | Yes, material will pool off and be thinner around edges to some degree
Is there any concern with moisture penetration if delaminated? | Yes
My PCB has components of different substrates. Is NanoProof compatible with metals and plastics? | Yes, with the exception of fluorinated materials
Can we reapply the material? What is suggested for rework or touch ups? | Yes, solvent can be used to clean questionable areas and then the material can be reapplied as desired. If appearance is not a concern then a simple coating reapplication should work.

## Slide 23
Aculon® is world class in surface modification technologies
NanoProof® 3 series offers direct replacements for 3M™ Novec™ Products
NanoProof® 3 series is readily available and easy to apply
SUMMARY
Ready to support you and to extend to other markets and products

## Slide 24
PERFORMANCE
SURFACE
SOLUTIONS
aculon.com
Questions

## Slide 25
 | 1720
Solids | Fluoroacrylate 0.1%
Solvent | 7100DL
Appearance | Clear
Density | 1.5 g/mL
Viscosity | <20 cP
Boiling Point | 61°C
Flash Point | None
Environmental | Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine
Shelf Life | 2 yrs (unopened container)
Thickness | <1 µm
Chem Resistance | Resists a variety of solvents and chemicals. Attacked by fluorosolvents and ketones.
Tg | -110°C
Therm. Stability | 200°C in air >3 hr
Contact Angles | WCA / OCA: 105° / 65°
Refractive Index | 1.39
Solder Thru Repairability | Yes
Cure | 135°C for 15 minutes
Removable | Not when cured
NANOPROOF® 3-001X vs NOVEC™ 1720
3-001X
Fluoroacrylate 0.1%
Aculon 3 Series Extender
Clear
1.5 g/mL
<20 cP
To be determined, Estimate 56-61°C
None
Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine
2 yrs in unopened package from manufacture date
<1 µm
Resists a variety of solvents and chemicals. Attacked by fluorosolvents and ketones.
~95°C from peak on DSC
In Process
WCA / OCA: 120° / 80°
n=1.376 @ 632.8 nm
Yes
None
Yes,

## Slide 26
 | 1902 | 1904 | 1908
Solids | Fluoroacrylate 2% | Fluoroacrylate 4% | Fluoroacrylate 8%
Solvent | Blend 7100/7200 |  | 
Appearance | Clear |  | 
Density | 1.43 g/mL |  | 
Viscosity | 0.81 cP | 1.11 cP | 2.2 cP
Boiling Point | 75°C |  | 
Flash Point | None |  | 
Environmental | Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine |  | 
Shelf Life | 2 yrs in unopened package from manufacture date |  | 
Thickness | 0.1-1 µm | 0.5-6 µm | 0.4-5 µm
Chem Resistance | Resists a variety of solvents/chemicals, dissolves in acetone |  | 
Tg | 44.5°C |  | 
Therm. Stability | 175°C for 24 hours |  | 
Contact Angles | WCA / OCA: 105° / 65° |  | 
Refractive Index | 1.39 |  | 
Solder Thru Repairability | Yes |  | 
Non-Flammability | Meets UL 94 V-0 |  | 
Coef. of Therm. Expansion | 70 µm/(m·°C) |  | 
Therm. Cond. | 0.1 W/m*K |  | 
Diel. Bd Strength | 2000 V/mil |  | 
Cure | None |  | 
NANOPROOF® 3 vs NOVEC™ 1900 SERIES
3-02 | 3-04 | 3-08
Fluoroacrylate 2% | Fluoroacrylate 4% | Fluoroacrylate 8%
Aculon 3 Series Extender |  | 
Light Green |  | 
1.5 g/mL |  | 
<20 cP |  | 
To be determined, Estimate 56-61°C |  | 
None |  | 
Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine |  | 
2 yrs in unopened package from manufacture date |  | 
0.2-2 µm | 0.25-2 µm | 0.25-4 µm
*Resists a variety of solvents/chemicals. Attacked by fluorosolvents and ketones |  | 
~95°C from peak on DSC |  | 
Stable in 175°C for 24 hours |  | 
WCA / OCA: 120° / 80° |  | 
n=1.376 @ 632.8 nm |  | 
Yes |  | 
Meets UL 94 V-0 |  | 
In Process |  | 
In Process |  | 
3600 V/mil |  | 
None |  | 

## Slide 27
 | 2704 | 2708
Solids | Fluoroacrylate 4% | Fluoroacrylate 8%
Solvent | 7200 and <5% PGMEA | 
Appearance | Yellow-Orange | 
Density | 1.4 g/mL | 
Viscosity | 1.75 cP | 4.9 cP
Boiling Point | 78°C | 
Flash Point | None | 
Environmental | Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine | 
Shelf Life | 2 yrs in unopened package from manufacture date | 
Thickness | 0.1-4 µm | 0.4-5 µm
Chem Resistance | Resists a variety of solvents/chemicals, dissolves in acetone | 
Tg | 53°C | 
Therm. Stability | 175°C for 24 hours | 
Contact Angles | WCA / OCA: 105° / 65° | 
Refractive Index | 1.39 | 
Solder Thru Repairability | Yes | 
Non-Flammability | Meets UL 94 V-0 | 
Coef. of Therm. Expansion | 88 µm/(m·°C) | 
Therm. Cond. | 0.1 W/m*K | 
Diel. Bd Strength | 2500 V/mil | 
Cure | None | 
NANOPROOF® 3 vs NOVEC™ 2700 SERIES
3-04 | 3-08
Fluoroacrylate 4% | Fluoroacrylate 8%
Aculon 3 Series Extender | 
Light Green | 
1.5 g/mL | 
<20 cP | 
To be determined, Estimate 56-61°C | 
None | 
Non-ozone depleting, low in toxicity, low in GMP, RoHS compliant and VOC exempt (per US EPA), contains no chlorine or bromine | 
2 yrs in unopened package from manufacture date | 
0.25-2 µm | 0.25-4 µm
*Resists a variety of solvents/chemicals. Attacked by fluorosolvents and ketones | 
~95°C from peak on DSC | 
175°C for 24 hours | 
WCA / OCA: 120° / 80° | 
n=1.376 @ 632.8 nm | 
Yes | 
Meets UL 94 V-0 | 
In Process | 
In Process | 
3600 V/mil | 
None |